|  |  |  |  |
| --- | --- | --- | --- |
|  | United Nations | ECE/TRANS/WP.29/GRE/2014/23 | |
| Description: _unlogo | **Economic and Social Council** | | Distr.: General  8 August 2014  Original: English |

**Economic Commission for Europe**

Inland Transport Committee

**World Forum for Harmonization of Vehicle Regulations**

**Working Party on Lighting and Light-Signalling**

**Seventy-second session**

Geneva, 20–22 October 2014

Item 4 (i) (iv) of the provisional agenda  
**1958 Agreement - Regulations**

**Other business – Any other business**

Proposal for Supplement 5 to the 01 series of amendments to Regulation No. 98 (Headlamps with gas-discharge light sources)

Submitted by the expert from the International Automotive Lighting and Light Signalling Expert Group (GTB)[[1]](#footnote-2)\*

The text reproduced below was prepared by the expert from the GTB to amend the requirements for dirt test mixture. The modifications to the existing text of the Regulation are marked in bold for new or strikethrough for deleted characters.

I. Proposal

*Annex 4, paragraph 1.2.1.1.*, amend to read:

1.2.1.1. Test mixture

1.2.1.1.1. For headlamp with the outside lens in glass:

The mixture of water and a polluting agent to be applied to the headlamp shall be composed of:

9 parts by weight of silica sand with a particle size of 0-100 μm,

1 part by weight of vegetal carbon dust **produced from** **~~(~~**beech wood**~~)~~** with a particle size of 0-100 μm,

0.2 parts by weight of NaCMC3, and

**5 parts by weight of sodium chloride (pure at 99 per cent),**

an appropriate quantity of distilled water, with a conductivity   
of ≤ 1 mS/m.

The mixture must not be more than 14 days old.

1.2.1.1.2. For headlamp with outside lens in plastic material:

The mixture of water and polluting agent to be applied to the headlamp shall be composed of:

9 parts by weight of silica sand with a particle size of 0-100 μm,

1 part by weight of vegetal carbon dust **produced from** **~~(~~**beech wood**~~)~~** with a particle size of 0-100 μm,

0.2 part by weight of NaCMC3,

**5 parts by weight of sodium chloride (pure at 99 per cent),**

13 parts by weight of distilled water with a conductivity of ≤ 1 mS/m, and

2 ± 1 parts by weight of surface-actant4.

The mixture must not be more than 14 days old.

II. Justification

The Regulations currently specify several test mixtures to simulate dirt during testing of lamps. As there is no reason to use different kinds of test mixtures it is proposed to amend the Regulations by introducing a uniform test mixture to be used for all the corresponding tests. In addition, to avoid misinterpretation the wording “beech wood**”** is replaced by “produced from beech wood”.

1. \* In accordance with the programme of work of the Inland Transport Committee for 2012–2016 (ECE/TRANS/224, para. 94 and ECE/TRANS/2012/12, programme activity 02.4), the World Forum will develop, harmonize and update Regulations in order to enhance the performance of vehicles. The present document is submitted in conformity with that mandate. [↑](#footnote-ref-2)