## Slide 1: UN Regulation No. 90 - CoP Document replacing GRVA-09-41 and GRVA-07-52
Additional Supporting Data
Submitted by the experts from CLEPA | Informal document GRVA-10-29 10th GRVA, 25-28 May 2021, Agenda item 10

## Slide 2: R90 CoP
Current Requirement
3.1.1. The machine shall be equipped with a disc brake of the fixed calliper type with a cylinder diameter of 60 mm and a solid (not ventilated) brake disc having a diameter of 278 ± 2 mm and a thickness of 12 mm ± 0.5 mm. A rectangular piece of the friction material with an area of 44 cm2 ± 0.5 cm2 and a thickness of at least 6 mm shall be attached to the backing plate
New Proposal
Keep 3.1.1. unchanged and add a new paragraph: 3.1.1.1. Alternatively the machine may be equipped with a disc brake and corresponding brake disc having a diameter of 278 ± 2 mm such as to allow a rectangular piece of the friction material with a surface area of 44cm2 ± 0.5cm2 and a thickness of at least 6 mm to be attached to the backing plates of the disc brake.
In this case the Registered Values of friction to be used for ongoing COP checks shall be established in accordance with the technical service by comparative tests using the same batch of friction material with the test hardware specified in 3.1.1 and the alternative hardware.
The applicant shall provide the values for the friction behavior resulting from the use of alternative test hardware in accordance with Annex 9 para 3.4.1 of this Regulation and the results shall be attached to the type-approval report
Components no longer commercially available

## Slide 3: Points of Discussion
1) Use of alternative type of brake calliper – Agreed
2) Use of alternative type of brake disc
  Vented rotor will result in lower EOS temperatures – will this detract from temperature spectrum experienced on approval tests
3) CLEPA position
  Annex 9 /3.2.2. specifies start temperatures no requirement for EOS
  Annex 9 /3.2.2. is an industry CoP test with surrogate parts not an approval test – no requirement for temperature matching
  However temperature spectrum still consistent with approval tests

## Slide 4: Annex 9 para 3.2.2 -Tests with Solid & Vented Discs
Cycle | No BrakeApps | IBT Deg c | Solid Disc | Vented Disc | % Diff
 |  |  | End of Cycle Temp – Deg c | End of Cycle Temp – Deg c | 
1 | 5 | 100 | 218 | 205 | -6%
2 | 5 | < 200 | 384 | 342 | -11%
3 | 5 | 200 | 385 | 342 | -11%
4 | 5 | < 300 | 433 | 375 | -13%
5 | 5 | 300 | 459 | 389 | -15%
6 | 3 | 250 | 265 | 260 | -2%
7 | 3 | 200 | 248 | 224 | -10%
8 | 3 | 150 | 214 | 194 | -9%
9 | 10 | 100 | 285 | 244 | -14%
10 | 5 | < 300 | 393 | 385 | -2%
11 | 5 | 300 | 484 | 406 | -16%
Total | 54 |  |  |  | 
 |  | Test Outcome |  |  | 
 |  | Mu Op1 | 0.494 | 0.524 | 6%
 |  | Mu Op2 | 0.463 | 0.490 | 6%
 |  | Mu Min | 0.348 | 0.360 | 3%
 |  | Mu Max | 0.530 | 0.542 | 2%

## Slide 5: Typical Temperatures on R90 HCV Approval Tests
Test No | Disc/ Drum | Disc/Drum Dia (mm) | DiscThk/ Drum width (mm) | Type 0 Test Test Temp (Deg. C) |  | Type 0 High Speed Test Temp (Deg. C) |  | Type 1 Fade (Deg. C) | Type II Fade (Deg. C) | Type III Fade (Deg. C)
 |  |  |  | Start | End | Start | End | Max | Max | Max
1 | Vent | 434 | 45 | 40 | 79 | 40 | 121 | 430 | 307 | N/A
2 | Vent | 434 | 45 | 40 | 72 | 40 | 116 | 387 | 331 | N/A
3 | Vent | 334 | 30 | 98 | 129 | 98 | 161 | 379 | 284 | N/A
4 | Drum | 410 | 178 | 90 | 140 | 96 | 188 | 392 | 322 | 358
5 | Vent | 377 | 45 | 97 | 143 | 96 | 155 | 394 | 341 | 372
Mean Values |  |  |  |  | 113 |  | 148 | 396 | 317 | 365
Range of Values on Annex 9 / 3.2.2 with vented discs |  |  |  |  | 100 > 406 Deg. c |  |  |  |  |