## Slide 1: UN Regulation No. 90 – CoP Annex 9 – 3.1.1 (HCV) Document replacing GRVA-09-41 and GRVA-07-52
Additional Supporting Data
Submitted by the experts from CLEPA | Informal document GRVA-10-29/Rev.1 10th GRVA, 25-28 May 2021, Agenda item 10

## Slide 2: The new proposal – Annex 9 / 3.1.1. - HCV
Current Requirement
3.1.1. The machine shall be equipped with a disc brake of the fixed calliper type with a cylinder diameter of 60 mm and a solid (not ventilated) brake disc having a diameter of 278 ± 2 mm and a thickness of 12 mm ± 0.5 mm. A rectangular piece of the friction material with an area of 44 cm2 ± 0.5 cm2 and a thickness of at least 6 mm shall be attached to the backing plate
Components no longer commercially available

## Slide 3: The new proposal – Annex 9 / 3.1.1. - HCV
New Proposal
Keep 3.1.1. unchanged and add a new paragraph: 3.1.1.1. Alternatively the machine may be equipped with a disc brake and corresponding brake disc having a diameter of 278 ± 2 mm such as to allow a rectangular piece of the friction material with a surface area of 44cm2 ± 0.5cm2 and a thickness of at least 6 mm to be attached to the backing plates of the disc brake.
In this case the Registered Values of friction to be used for ongoing COP checks shall be established in accordance with the technical service by comparative tests using the same batch of friction material with the test hardware specified in 3.1.1 and the alternative hardware.
The applicant shall provide the values for the friction behavior resulting from the use of alternative test hardware in accordance with Annex 9 para 3.4.1 of this Regulation and the results shall be attached to the type-approval report
Removes restriction on type of
Brake calliper
Brake disc
Change of hardware requires back to back tests to determine effect (if any) on Registered Values
Existing Registered Friction Values either re-confirmed or new values established

## Slide 4: Points of Discussion
1) Use of alternative type of brake calliper – Agreed
2) Use of alternative type of brake disc
  Vented rotor will result in lower EOS temperatures – will these be lower than temperature range experienced on approval tests ?
CLEPA position
  Annex 9 /3.2.2. specifies start temperatures - no requirement for EOS
  Annex 9 /3.2.2. is an industry CoP test with surrogate parts, not an approval test – no requirement for temperature matching
  EOS temperature is a product/test variable not a control parameter

## Slide 5: Typical EOS temperatures on R90 HCV Approval Tests
Test No | Disc/Drum | Diameter (mm) | Thick / Width (mm) | Type 0 EOS (Deg. C) | Type 0 HS EOS (Deg. C) | Type 1 Max (Deg. C) | Type 11 Max (Deg. C) | Type 111 Max (Deg. C)
1 | Disc – Vent | 334 | 30 | 129 | 161 | 379 | 284 | N/A
2 | Disc - Vent | 377 | 45 | 143 | 155 | 394 | 341 | 372
3 | Disc - Vent | 434 | 45 | 79 | 121 | 430 | 307 | N/A
4 | Disc - Vent | 434 | 45 | 72 | 116 | 387 | 331 | N/A
5 | Drum | 410 | 178 | 140 | 188 | 392 | 322 | 358
Mean Values |  |  |  | 113 | 148 | 396 | 317 | 365
Overall Mean Range |  |  |  | 113 > 396 Deg. C |  |  |  | 

## Slide 6: Annex 9 – 3.2.2. Tests with Solid & Vented Discs
 |  | Friction Material A – Higher Mu / Low Fade |  |  | Friction Material B – Lower Mu / Higher Fade * |  | 
Cycle | IBT – Deg C | Solid | Vented | % Diff | Solid | Vented | % Diff
1 | 100 | 218 | 205 | 6% | 132 | 96 | 27%
2 | <200 | 384 | 342 | 11% | 295 | 212 | 28%
3 | 200 | 385 | 342 | 11% | 336 | 270 | 20%
4 | <300 | 433 | 375 | 13% | 347 | 306 | 12%
5 | 300 | 459 | 389 | 15% | 343 | 325 | 6%
6 | 250 | 265 | 260 | 2% | 235 | 248 | 5%
7 | 200 | 248 | 224 | 10% | 211 | 206 | 2%
8 | 150 | 214 | 194 | 9% | 178 | 170 | 5%
9 | 100 | 285 | 244 | 14% | 230 | 194 | 16%
10 | <300 | 393 | 385 | 2% | 372 | 320 | 14%
11 | 300 | 484 | 406 | 16% | 370 | 343 | 7%
* Average of 6 tests on each brake disc form

## Slide 7: Temperature Profiles
Chart: Test Procedure
| Type 0 | Type 0 High Speed | Type 1 Fade | Type 11 Fade | Type 111 Fade | Annex 9/3.2.2 - Vented Rotor - Material A | Annex 9/3.2.2 - Vented Rotor - Material B
High | 143 | 188 | 430 | 341 | 372 | 100 | 85
Low | 40 | 40 | 379 | 284 | 358 | 406 | 365
Mean | 113 | 148 | 396 | 317 | 365
Annex 9 / 3.2.2. tests with vented rotors broadly cover the temperature spectrum seen on R90 Approval tests

## Slide 8: Registered Friction Values
 | Friction Material A – High Mu/ Low Fade |  | Friction Material B – Lower Mu/ Higher Fade * | 
 | Solid Disc | Vented Disc | Solid Disc | Vented Disc
Mu Op 1 | 0.49 | 0.52 | 0.31 | 0.30
Mu Op 2 | 0.46 | 0.49 | 0.39 | 0.39
Mu Min | 0.35 | 0.36 | 0.17 | 0.2
Mu Max | 0.53 | 0.54 | 0.43 | 0.43
* Average of 6 tests on each disc form
Friction values not significantly changed by disc form
Characterisation of products not affected by disc form